

**Commercial offer of Uzbek enterprises’ products**

**to foreign customers**

**Information about the company:**LLC "Urganch Bakhmal" - was founded in 2005 and today is a successful and dynamic company which is based on new technologies and equipment of the leading companies in the world. The company for the first time in Uzbekistan in 2012, the company launched production of flannel. Enterprise has and international quality certificate ISO - 9001: 2009.

The main purpose of "Urganch Bakhmal" is to create a competitive product that meets all modern requirements of quality, range improvement, maximum consumer satisfaction.

**List of products :**

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **№** | **Fabric Name** | | **Price for 1 n / m in US dollars** | **Fabric width in cm (± 2)** | **Weight g / m² (± 5)** | **The density of 1 cm²** | |
| the basis | woof |
| 1 | Cotton bleached cloth | | 0.38 | 150 | 100 | 20 | 11 |
| 2 | Cotton fabric | | 0.39 | 150 | 100 | 20 | 11 |
| 3 | Cotton polugrunt fabric | | 0.41 | 150 | 100 | 20 | 11 |
| 4 | Cotton cloth stuffed | | 0.44 | 150 | 100 | 20 | 11 |
| 5 | cotton fabric stuffed for bed linen | | 0.44 | 150 | 100 | 20 | 11 |
| 6 | Poplin | | 0.83 | 150 | 105 | 25 | 22 |
| 7 | Headscarf | | 0.41 | 160 | 100 | 18 | 12 |
| 8 | Handkerchief | Men | 0.58 | 160 | 110 | 22 | 14 |
|  | Woman | 0.54 | 160 | 110 | 22 | 14 |
| 9 | Active printing | | 1.15 | 160 | 140-150 | 39 | 26 |
| 10 | Cotton Flannel fabric (negligence, baby, shirting) | | 0.60 | 90 | 160 | 20 | 17 |
| 11 | Brocade (satin weave) | All types | 1.43 | 160 | 160 | 37 | 28 |

**Packaging:** At the buyer's request

**Terms of delivery:** Inventory

**Payment Terms:** Prepayment 100%

**Address:** Uzbekistan, Tashkent, 100047, Amir Temur Street 4,

Tel.: 2363570, 2337494 Fax: 1503101

E-mail: export@chamber.uz

Web: www.chamber.uz